Qualification Result Summary of 14x14 LQFP Using G631HQ/3230 at Amkor Philippines

| QUALIFICATION PLAN / STATUS |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | result |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 3 x 45 | Pass |
| Unbiased HAST (uHAST)* | JEDEC JESD22-A118 | 3 x 45 | Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3 x 45 | Pass |
| Solder Heat Resistance (SHR)* | JEDEC/IPC J-STD-020 | 3 x 11 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1 x 45 | Pass |
| Electrostatic Discharge Field-Induced Charged Device Model (FICDM) | JEDEC JESD22-C101 | 3/voltage | Pass 250V |

*Preconditioned per JEDEC/IPC J-STD-020