| QUALIFICATION PLAN# 9290 |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Expected Completion Date |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 1*32 3*45 1*45 3*77 | Pass Pass Pass Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3*77 3*77 3*77 3*77 | Pass Pass Pass Pass |
| Early Life Failure (ELF) | MIL-STD-883 Method 1015 | 3*800 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1*32 2*77 1*77 1*45 1*77 1*77 | Pass Pass Pass Pass Pass Pass |
| Latch-Up | JEDEC JESD78 | 6 | Pass 100mA |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JDS-001-2011 | 3/voltage | Pass 2500V |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Pass 750V |

*Preconditioned per JEDEC/IPC J-STD-020