Qualification Results Summary of REF43 Standard Space Level Change of Wafer Diameter and Fab Site

| QUALIFICATION PLAN/STATUS |  |  |  |
| --- | --- | --- | --- |
| TEST | SPECIFICATION | SAMPLE SIZE | RESULTS |
| Total Ionizing Dose RHA Level = 30, 50, & 100 K Rads (Si) | MIL-STD-883, Test Method 1019, Condition A (High Dose Rate) | 32 | 30K Rads – pass 50 K Rads – pass 100 K Rads – pass |
| High Temperature Operating Life Test | MIL-STD-883, Test Method 1015 | 45(0) Per wafer lot | In-process, Expected Completion Date November, 2015. |