Qualification Results Summary of the Wafer Level Capping of the ADXL103, ADXL203, ADXL204, ADXL212 and the ADXL213

| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Early Life Failure Rate (ELFR) | Mil-Std-883 Method 1015 | 2000 | Pass |
| Group D Sub-Group 4 | Mil-Std-883 Method 5005 | 3x17 | Pass |
| Group D Sub-Group 6 | Mil-Std-883 Method 5005 | 3X5 | Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3x77 | Pass |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 12x77 | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 | 4x77 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1x200 9x77 | Pass |
| Low Temperature Storage Life (LTS) | JEDEC JESD22-A119 | 6x77 | Pass |
| Random Drop | AEC-Q100 Test G5 | 3X45 | Pass |
| Solder Heat Resistance (SHR)* | JEDEC/IPC J-STD-020 | 3x30 | Pass |

*Preconditioned to JEDEC Std-20 MSL 3