## Slide 1: 2M Thick with old Poly (BL130) to 2M Thick with new Poly (8124ER) Sine Wave HVE Characterization @ 85C & 85%RH
Reliability GROUP
07/07/2016

## Slide 2: HVE Testing Details
Test Vehicles:
  (Lot #AK15389.7 and DC 1429)  2M Thick with BL130 Polyimide
  (Lot #3355863.1 and DC 1552)  2M Thick with 8124ER Polyimide
Sine wave HVE Testing
Temp = +85C and 85%RH
Stress Voltages: 3kVac, 2.5kVac, 2.0kVac, 1.5kVac and 1kVac
23 units per stress voltage
Package: 20L SOIC_W
Maximum Continuous Working Voltage Supporting a 50-Year: 400Vrms (per datasheet)

## Slide 3: Raw Weibull Distributions
Old Polyimide BL130
New Polyimide 8124ER

## Slide 4: T50 Lifetime Curve (1/Y2 Weight)
Old Polyimide BL130
New Polyimide 8124ER

## Slide 5: 1% TTF Lifetime Curve (1/Y2 Weight)
Old Polyimide BL130
New Polyimide 8124ER

## Slide 6: 1ppm Lifetime Curve (1/Y2 Weight)
New Polyimide 8124ER
Old Polyimide BL130

## Slide 7: New Polyimide 8124ER – Combined Lifetime Curves