PCN 17_0061

Qualification Results

| TEST NAME | SPECIFICATION | SAMPLE SIZE | RESULTS |
| --- | --- | --- | --- |
| High Temp Operating Life | 500 Hrs @ +125 C T-junction minimum | 16 (0) | Pass |
| Temperature Cycle* | ###### JESD22, Method A104-A ###### Condition G -40C to +125C. 500 Cycles | 16 (0) | Pass |

* These samples were subjected to preconditioning (per J-STD-020 Level 5) prior to the start of stress test. Level 5 preconditioning consist of the following: Bake: 24 hrs @ +125°C, Unbiased Soak: 72 hr @+30°C, 60%RH, Reflow: 3 passes through an oven with a peak temperature of + 240°C.