Qualification Results Summary of

ADP2119/20 Die Revision B Qualification

| QUALIFICATION RESULT |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Result |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JS-002 | 3/voltage | PASS ±TC1250 |
| Electrostatic Discharge Human Body Model | JEDEC JESD22-A114 | 3/voltage | PASS ±4000V |
| Latch-Up | JEDEC JESD78 | 15 | PASS |
| Solder Heat Resistance (SHR)1 | JEDEC J-STD-020 | 30 | PASS |

1Preconditioned per JEDEC J-STD-020 Level 3