Qualification Results Summary of Revision to Thickness of Polyimide and Redistribution Layers for ADN8833 and ADN8834 in WLCSP

| QUALIFICATION PLAN |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size (lot*sample) | Results |
| Temperature Cycle (TC) -40C to +125C (1 cycle/hour) 500 cycles | JEDEC JESD22-A104 | 3*77 | Pass |
| Unbiased HAST (UHAST) 130C / 85% RH 96 hours | JEDEC JESD22-A118 | 3*25 | Pass |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JS-002 | 1*18 3/voltage | Pass |