Qualification Results Summary for

ADE7932/ADE7933 Die Revision

| QUALIFICATION PLAN / STATUS |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Results |
| High Temperature Operating Life (HTOL)*2 | JEDEC JESD22-A108 | 9 x 77 | Pass |
| Highly Accelerated Stress Test (HAST)*1 | JEDEC JESD22-A110 | 9 x 77 | Pass |
| Temperature Cycle (TC)*1 | JEDEC JESD22-A104 | 9 x 77 | Pass |
| Unbiased HAST*1 | JEDEC JESD22-A118 | 9 x 77 | Pass |
| High Temperature Storage Life (HTSL)1 | JEDEC JESD22-A103 | 9 x 77 | Pass |
| Solder Heat Resistance (SHR)*1 | JEDEC/IPC J-STD-020 | 1 x 30 | Pass |
| Latch-Up1 | JEDEC JESD78 | 1 x 18 | Pass ±200mA @ +5.445V |
| Electrostatic Discharge Human Body Model1 | ESDA/JEDEC JS-001 | 3/voltage | Pass ±1000V |
| Electrostatic Discharge Field-Induced Charged Device Model1 | JEDEC JS-002 | 3/voltage | Pass ±1250V |

*Preconditioned per JEDEC/IPC J-STD-020

1 Electrical test was performed at Room