AD6676 Assembly Bumping Site Transfer from Amkor to TSMC

Qualification Results Summary of 80-WLCSP

Bumping to TSMC

| QUALIFICATION PLAN / STATUS |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Results |
| High Temperature Operating Life (HTOL) | JEDEC JESD22-A108 | 3*45 6*32 | Pass |
| Highly Accelerated Stress Test (HAST) | JEDEC JESD22-A110 | 9*32 | Pass |
| Temperature Cycle (TC) | JEDEC JESD22-A104 | 9*45 | Pass |
| Temperature/Humidity/Bias (THB) | JEDEC JESD22-A101 | 9*45 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 3*45 | Pass |