Qualification Results Summary

of AD9833WBRMZ-REEL

| QUALIFICATION PLAN |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Results |
| Electrostatic Discharge Field-Induced Charged Device Model (corner pins) | JEDEC JS-002 | 3/voltage | Pass ±750V |
| Electrostatic Discharge Field-Induced Charged Device Model (all pins) | JEDEC JS-002 | 3/voltage | Pass ±750V |
| Electrostatic Discharge Human Body Model | JEDEC JESD22-A114 | 3/voltage | Pass ±2500V |
| Latch-Up | JEDEC JESD78 | 1 x 15 | Pass |
| Highly Accelerated Stress Test (HAST)1 | JEDEC JESD22-A110 | 3 x 82 | Pass |
| Unbiased Highly Accelerated Stress Test (uHAST)1 | JEDEC JESD22-A118 | 3 x 82 | Pass |
| High Temperature Operating Life (HTOL)1 | JEDEC JESD22-A108 | 1 x 82 | Pass |
| High Temperature Storage Life (HTS) | JEDEC JESD22-A103 | 1 x 82 | Pass |
| Temperature Cycle Test (TCT)1 | JEDEC JESD22-A104 | 3 x 82 | Pass |
| Wire Bond Pull | MIL-STD-883 M2011 | 3 x 5 | Pass |
| Solder Heat Resistance (SHR)1 | JEDEC J-STD-020 | 3 x 16 | Pass |
| Solderability | JEDEC J-STD-002 | 1 x 15 | Pass |

1Preconditioned per JEDEC J-STD-020 Level 3