Qualification Results Summary of the AD5535B 2-Layer Laminate Design 2.1 NBOT Qualification

| QUALIFICATION PLAN - 14901 |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Expected Completion Date |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 3 x 77 | Passed |
| Unbiased Highly Accelerated Stress Test (uHAST)* | JEDEC JESD22-A118 | 3 x 77 | Passed |
| Low Temperature Operating Life (LTOL) | JEDEC JESD22-A108 | 3 x 77 | Passed |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 3 x 77 | Passed |
| Temperature/Humidity/Bias (THB)* | JEDEC JESD22-A101 | 3 x 77 | Passed |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1 x 77 | Passed |
| Solder Heat Resistance (SHR)* | JEDEC/IPC J-STD-020 | 3 x 11 | Passed |
| Latch-up Test | JESD78 | 3/level | Passed |
| Electrostatic Discharge Human Body Model | JS-001 | 3/voltage | Passed ±2.5kV |
| Electrostatic Discharge Field-Induced Charged Device Model | JS-002 | 3/voltage | Passed ±250V |

*Preconditioned per JEDEC/IPC J-STD-020