Qualification Plan Summary

of ADuM7701 and ADuM7703

| QUALIFICATION PLAN |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Result |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JS-002 | 3/voltage | Pass ±1500V |
| Electrostatic Discharge Human Body Model | JEDEC JESD22-A114 | 3/voltage | Pass ±4000V |
| Latch-Up | JEDEC JESD78 | 1 x 15 | Pass |