| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL) | JEDEC JESD22-A108 | 9 lots 45 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 3 lots of 45 | Pass |
| Latch-Up | JEDEC JESD78 | 6 | Pass |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JDS-001-2011 | 3/voltage | Pass 500V |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Pass 500V |

ADCMP402 Qualification Data