## Slide 1: Qualification of the Transfer of the BIPOLAR SV process from ADWIL ADLK 8”

## Slide 2: Overview of Qualification
Qualification of the BIPOLAR SV process in ADLK will include Device Level Testing and Product Level Testing.
Parts to be transferred are:
  OP297
  OP497

## Slide 3: OP297 Product Level Qualification Plan
Qualification will be performed per Analog Devices specification ADI-0012. ADI0012 is the procedure for qualification for New or Revised Processes or Products. The Qualification Report will be available after completion, upon request.
Sample size typically 77/lot
1 Preconditioned Per JEDEC/IPC J-STD-020
OP297 Qualification |  |  | 
TEST | Standard | CONDITIONS | Quantities
High Temperature Operating Life1 | JEDEC JESD22-A108 | 1000hrs @ 125C biased | 1x77
Early Life Failure | JEDEC JESD22-A108 | 48hrs @125C biased | 1x667
Highly Accelerated Stress Test (HAST) 1 | JEDEC JESD22-A110 | 96hrs @ 85%RH 131C biased | 3x77
Temperature Cycle1 | JEDEC JESD22-A104 | 500cycles -65C/+150C | 1x77
Autoclave1 | JEDEC JESD22-A102 | 96hrs @ 100%RH 121C unbiased | 1x77
High Temperature Storage | JEDEC JESD22-A103 | 1000hrs @ 150C | Substitute Data
Latch-Up | JEDEC Standard 78 | +25C Biased single duration 100/99mA | 1x6
Electrostatic Discharge Human Body Model | ESD Association STM5.1-2001 | Std Sample 1 Zap per polarity p/f 1000V/999V | 1x24*
Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 | All pins 3 zaps per polarity p/f 500V/499V | 1x18*
*ESD HBM & FICDM will meet existing product process requirements

## Slide 4: OP497 Product Level Qualification Plan
Qualification will be performed per Analog Devices specification ADI-0012. ADI0012 is the procedure for qualification for New or Revised Processes or Products. The Qualification Report will be available after completion, upon request.
Sample size typically 77/lot
1 Preconditioned Per JEDEC/IPC J-STD-020
OP497 Qualification |  |  | 
TEST | Standard | CONDITIONS | Quantities
High Temperature Operating Life1 | JEDEC JESD22-A108 | 1000hrs @ 125C biased | Substitute Data
Early Life Failure | JEDEC JESD22-A108 | 48hrs @125C biased | Substitute Data
Highly Accelerated Stress Test (HAST) 1 | JEDEC JESD22-A110 | 96hrs @ 85%RH 131C biased | Substitute Data
Temperature Cycle1 | JEDEC JESD22-A104 | 500cycles -65C/+150C | Substitute Data
Autoclave1 | JEDEC JESD22-A102 | 96hrs @ 100%RH 121C unbiased | Substitute Data
High Temperature Storage | JEDEC JESD22-A103 | 1000hrs @ 150C | Substitute Data
Latch-Up | JEDEC Standard 78 | +25C Biased single duration 100/99mA | 1x6
Electrostatic Discharge Human Body Model | ESD Association STM5.1-2001 | Std Sample 1 Zap per polarity p/f 1000V/999V | 1x24*
Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 | All pins 3 zaps per polarity p/f 500V/499V | 1x18*
*ESD HBM & FICDM will meet existing product process requirements