| Package | Assembly Site | Autoclave1 121°C, 100%RH, 2 atm, 96 hrs | HAST1 130C 85%RH 2atm, Biased | HTS1 150°C, 1000 hrs | Temp Cycle1 -65°C to 150°C, 500 cycles | SHR (Solder Heat Resistance) |
| --- | --- | --- | --- | --- | --- | --- |
| SOIC_N | Carsem M | Pass | Pass | Pass | Pass | Pass |
|  | TOTAL: | 0 fails/1232 samples | 0 fails/ 385 samples | 0 fails/847 samples | 0 fails/1232 samples | 0/366 |

QUALIFICATION RESULTS: PCN 10_0356

1 Parts subjected to preconditioning per J-STD-0020, MSL 1, 3 or 5 with peak reflow temperature of 260°C prior to stress