| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 308 | Pass |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 308 | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 | 308 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 154 | Pass |
| Solder Heat Resistance (SHR)* | ADI-0049 | 63 | Pass |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Pass 500V |

*Preconditioned per JEDEC/IPC J-STD-020