	QUALIFICATION SUMMARY

	Test
	Conditions
	Sample Size
	Results

	Latch-Up
	JEDEC JESD78
	6
	Pass

	Electrostatic Discharge

Human Body Model
	ANSI/ANSI/ESDA/JEDEC JS-001-2010
	3
	Class 2
Passed 2000V

	Electrostatic Discharge

Field-Induced Charged Device Model
	JEDEC JESD22-C101
	3
	Pass 250V


