| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Solder Heat Resistance (SHR)* for 8-MINI_SO | ADI-0049 | 30 | Pass |
| Solder Heat Resistance (SHR)* for 8-LFCSP | ADI-0049 | 30 | Pass |
| Latch-Up (8-MINI_SO) | JEDEC JESD78 | 6 | Pass |
| Electrostatic Discharge Human Body Model (8-LFCSP) | ESDA/JEDEC JDS-001-2011 | 3/voltage | Pass 6kV |
| Electrostatic Discharge Machine Model (8-LFCSP) | JEDEC JESD22-A115 | 3/voltage | Pass 200V |
| Electrostatic Discharge Field-Induced Charged Device Model (8-MINI_SO) | JEDEC JESD22-C101 | 3/voltage | Pass 1.25kV |
| Electrostatic Discharge Field-Induced Charged Device Model (8-LFCSP) | JEDEC JESD22-C101 | 3/voltage | Pass 1.25kV |

Qualification Plan #9865 – AD8657 Die Revision Ya at TSMC Fab 10 Qualification

*Preconditioned per JEDEC/IPC J-STD-020