| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 9x45 | Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 9x45 | Pass |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 9x45 | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 | 9x45 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 3x45 | Pass |
| Solder Heat Resistance (SHR)* | ADI-0049 | 1x30 | Pass |
| Latch-Up | JEDEC JESD78 | 6 | Pass |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JDS-001-2011 | 3/voltage | Pass 2500V |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Pass 1250V 28-SOIC_W |
|  |  |  | Pass 750V 28-PDIP |
|  |  |  | PASS 500V 28-CERDIP |

*Preconditioned per JEDEC/IPC J-STD-020 MSL 3