PCN12_0239

| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 8x77 | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 | 8x77 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 3x77 | Pass |
| Solder Heat Resistance (SHR) | ADI-0049 | 7x15 1x30 | Pass |

*Preconditioned per JEDEC/IPC J-STD-020