AD9272/AD9273 rev. R3

| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Results |
| Latch-Up | JEDEC JESD78, Class I | 6 | Pass |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JDS-001-2011 | 3/voltage | Pass ±2000V |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage, 100-TQFP_EP | Pass ±750V |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage, 144-CSP_BGA | Pass ±1250V |
| Electrostatic Discharge Machine Model | JEDEC JESD22-A115 | 3/voltage | Pass ±100V |