PCN 13_0070
Qualification Summary

| Test | Conditions | Sample Size | Result |
| --- | --- | --- | --- |
| Temperature Cycle* | ###### JESD22, Method A104 ###### Condition G -40C to +125C. 1000 cycles Data points at 200, 500 and 1000 cycles. | 32 | Pass |
| High Temperature Operating Life* | ###### JESD22, Method A108 125°C TA/TC 500 Hr. | 16 | Pass |
| Unbiased HAST | ###### JESD22, Method A110 ###### 130°C / 85% RH 2atm ###### Unbiased 96Hr. | 16 | Pass |

*Preconditioned Per JEDEC/IPC J-STD-020 prior to this stress test.