| QUALIFICATION PLAN #10524 |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Expected Completion Date |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 1*77 | Nov 2013 |
|  |  | 1*77 | Nov 2013 |
| Early Life Failure (ELF) | MIL-STD-883, Method 1015 | 3*667 | Nov 2013 |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1*45 | Oct 2013 |
|  |  | 1*45 | Oct 2013 |
| Latch-Up | JEDEC JESD78 | 6 | Oct 2013 |
|  |  | 6 | Oct 2013 |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JDS-001-2011 | 3/voltage | Oct 2013 |
|  |  | 3/voltage | Oct 2013 |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Oct 2013 |
|  |  | 3/voltage | Oct 2013 |
| Electrostatic Discharge Machine Model | JEDEC JESD22-A115 | 3/voltage | Oct 2013 |
|  |  | 3/voltage | Oct 2013 |
| Electrostatic Discharge 15kV IEC HBM | IEC 6100-4-2 | 3/voltage | Nov 2013 |
|  |  | 3/voltage |  |

*Preconditioned per JEDEC/IPC J-STD-020