QP#10511: AD5748_AD5750_AD5750-1_AD5750-2 Die Rev and Package Qualification

| QUALIFICATION PLAN# 10511 /INCOMPLETE |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 7 x 45 3 x 77 | Pass Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3 x 77 3 x 77 | Pass Expected in May |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 3 x 77 3 x 77 | Pass Expected in May |
| Autoclave (AC)* | JEDEC JESD22-A102 | 3 x 77 3 x 77 | Pass Expected in May |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 1 x 45 1 x 45 | Pass Expected in April |
| Solder Heat Resistance (SHR)* | JEDEC/IPC J-STD-020 | 1 x 30 | Pass |
| Latch-Up | JEDEC JESD78 | 3 | Pass |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JS-001 | 3/voltage | Pass __3KV |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Pass _1.25KV |

*Preconditioned per JEDEC/IPC J-STD-020