ADI PCN 13_0217

| ADXRS64x Die Revision R.8 QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 3x77 | Pass |
| Latch-Up | JEDEC JESD78 | 6 | Pass |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JDS-001-2011 | 3/voltage | Pass 2000V |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Pass 500V |

*Preconditioned per JEDEC/IPC J-STD-020