## Slide 1: Bill of Materials
 | SCM | SCC | Remarks
Die Attach | Hitachi EN4900 | Hitachi EN4900 | Same BOM
Wire type | Gold MKE UR2 | Gold MKE UR2 | 
Mold Compound | Hitachi CEL9220 | Hitachi CEL9220 | 
Lead Finish | NiPdAu | NiPdAu |