ADP5050/52 Die Revision Qualification

| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Specification | Sample Size | Results |
| Latch-Up | JEDEC JESD78 | 6 | Pass |
| Electrostatic Discharge Human Body Model | ESDA/JEDEC JS-001 | 3/voltage | Pass +/-3500V |
| Electrostatic Discharge Field-Induced Charged Device Model | JEDEC JESD22-C101 | 3/voltage | Pass +/-1250V |