Qual Summary for AD8028 
	QUALIFICATION RESULTS

	Test
	Conditions
	Sample Size
	Results

	High Temperature Operating Life (HTOL)*


	JEDEC JESD22-A108
	9 x 45
	Pass

	Highly Accelerated Stress Test (HAST)*
	JEDEC JESD22-A110
	8 x 77
1 x 45
	Pass

	Temperature Cycle (TC)*
	JEDEC JESD22-A104
	9 x 77
	Pass

	Autoclave (AC)*
	JEDEC JESD22-A102
	9 x 77
	Pass

	High Temperature Storage Life (HTSL)
	JEDEC JESD22-A103
	7 x 77
2 x 45
	Pass

	SHR (Solder Heat Resistance)*
	ADI-0049
	1 x 30
	Pass

	Electrostatic Discharge

Human Body Model
	ESD Association

STM5.1-2007
	1 x 18
	Pass ±8000V

	Electrostatic Discharge

Field-Induced Charged Device Model
	ESD Association

STM5.3.1-1999
	1 x 18
	Pass ±2000V1

	
	
	1 x 18
	Pass ±1500V2

	Electrostatic Discharge Machine Model
	JESD22-A115
	1x18
	Pass

±400V


*Preconditioned per JEDEC/IPC J-STD-020
1 Test was conducted on AD8028 in 8L-SOIC_nb

2 Test was conducted on AD8028 in 10L-mSOIC
