Qualification Results Summary for Addition of a Polyimide Layer to the AD8188 and AD8189
	QUALIFICATION RESULTS

	Test
	Conditions
	Sample Size
	Results

	Highly Accelerated Stress Test (HAST)*
	JEDEC JESD22-A110
	9 x 32
	Pass

	Temperature Cycle (TC)*
	JEDEC JESD22-A104
	2 x 77
5 x 45

2 x 32


	Pass

	Autoclave (AC)*
	JEDEC JESD22-A102
	2 x 77
6 x 45

1 x 32
	Pass


*Preconditioned per JEDEC/IPC J-STD-020
